Functional Materials Manufacturing, Inc.

Ceramic Cutting Tools

Increasing Productivity

Through Innovation

555 Gore Road

Kingston, Onatrio, Canada K7L 5H6

Tel: (613)484-0603

Fax: (613)533-6610

INTRODUCTION

FMM offers a broad range of high performance ceramic cutting tools. Ceramics possess high melting points, high hardness and excellent wear resistance and ability to retain mechanical properties at high temperatures thus making them highly suitable for high speed machining. Interest in ceramics as a high-speed cutting tool for machining of most common metals and alloys has increased over the decade, due to potentials to increase the productivity of metal cutting operations by an order of magnitude. Our silicon nitride and SiAlON based tools have the best combination of hardness and toughness allowing a major increase in cutting speed. For example, it has been possible to increase the cutting speeds form ~200 sm/min for tool steel to over 2600 sm/min for silicon nitride cutting tools.

Most significant application of ceramic cutting tool grades FM02, FM55C and FM73C is in machining of hard steel and iron (up to 64 HRC). Also, roughing and finishing can be performed in one step operation.

Due to continuous research and advancement in cutting tool materials, new grades of ceramic cutting tools based on silicon nitride and titanium carbide for even higher cutting speeds are being introduced.

This catalogue offers FMM’s state of the art ceramic cutting tools renowned for their high quality and versatility.

| TABLE OF CONTENTS | PAGE |
| --- | --- |
| 1. Ceramic Cutting Tool Grades................................................................... | 3 |
| 2. Insert Identification.................................................................................... | 4 |
| 3. Ceramic Inserts for Turning and Boring................................................. | 5 |
| 4. Technical Data............................................................................................ | 8 |
| 4.1. Recommendations for Turning | 19 |
| 4.2. Definitions of Terms and Formulas | 20 |
| 4.3. Machining Recommendations for Turning 4.4. Suggestions for the Ceramic User 4.5. Feedrate Selection for Turning with Ceramic Cutting Tools 4.6. Basic Formulas 4.7. Edge Preparation | 21 27 28 29 30 |

| Grade | Composition | Application |
| --- | --- | --- |
| FMA | Aluminum Oxide, pure | Fine finishing of soft cast irons and steels with hardness of up to 35 HRC (330 BHN) |
| FMAZ1 | Aluminum Oxide-Zirconium Oxide (10 vol %) | Finishing of gray cast iron, carbon steel, alloy steel with hardness of up to 38 HRC (350BHN) |
| FMAZ2 | Aluminum Oxide-Zirconium Oxide (20 vol %) | Roughing of gray cast iron, ductile cast iron, carbon steel, alloy steel and tool steel with hardness of up to 38 HRC (350 BHN) |
| FMAZ3 | Aluminum Oxide-Titanium Carbide (30 wt %) | Roughing and finishing hard steel with hardness of up to 64 HRC (740 BHN) |
| FM02 | Silicon Nitride with Metal Oxides | Roughing, turning and milling of gray cast iron |
| FM55C | Silicon Nitride Based Ceramics | Roughing, turning and milling of gray cast iron |
| FM64C | Silicon Nitride Based Ceramics | Roughing, turning and milling of gray cast iron |
| FM73C | Silicon Nitride Based Ceramics | Roughing, turning and milling of gray cast iron |
| FMYC | SiAlON Based Ceramics | Roughening and finishing of cast iron, carbon steel, alloy steel and tool steel |
| FMTCN | Titanium Carbide-Based Cermet |  |

C-Rhombic (Diamond 80) D- Rhombic (Diamond 55) R-Round S-Square T-Triangle

1 INSERT SHAPE

- C

- D

- R

- S

- T

N - Without Hole

4 INSERT TYPE

N - 0  P - 11 

2 RADIUS

| G | +/- I.C. .001 In .025mm | +/- B .001 In .025 mm | +/- T .005 In .13mm |
| --- | --- | --- | --- |
| 3 TOLERANCE |  |  |  |

3

G

4

N

5

12

6

03

1

S

2

P

7

08

| 5 INSERT SIZE |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| I.C. Inch | C | D | R | S | T |
| 1/4 | 06 | 07 | - | 06 | 11 |
| 3/8 | 09 | 12 | 09 | 09 | 16 |
| 1/2 | 12 | 15 | 12 | 12 | 22 |
| 5/8 | 16 | 19 | 15 | 15 | 27 |
| 3/4 | 19 | 23 | 19 | 19 | 33 |
| 1 | 25 | 31 | 25 | 25 | 44 |

| 6 THICKNESS |  |
| --- | --- |
| Inch | Symbol |
| 1/8 | 3 |
| 3/16 | 4 |
| 1/4 | 6 |
| 5/16 | 7 |
| 3/8 | 9 |

| 7 RADIUS |  |
| --- | --- |
| Inch | Symbol |
| 1/64 | 4 |
| 1/32 | 8 |
| 3/64 | 12 |
| 1/16 | 16 |
| 1/8 | 32 |

CNG 80 diamond negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  | All Grades |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | FMA | FMAZ1 | FMAZ2 | FMAZ3 | FM FM FM FM FM 02 C55 64C 73C 1515 |
| CNG-432 CNG-433 | CNGN 120408 CNGN 120412 | T-01 T-02 | 1/2 1/2 | 3/16 3/16 | 1/32 3/64 |   |  |  |   | ○  ○ |
| CNG-452 CNG-453 CNG-453 CNG-454 CNG-454 | CNGN 120708 CNGN 120712 CNGN 120712 CNGN 120716 CNGN 120716 | T-02 T-02 T-03 T-02 T-03 | 1/2 1/2 1/2 1/2 1/2 | 5/16 5/16 5/16 5/16 5/16 | 1/32 3/64 3/65 1/16 1/16 | ○ ○ ○ ○ ○ |   |   |   |  |
| CNG- 542 CNG- 543 CNG -544 | CNGN 160608 CNGN 160612 CNGN 160716 | T-02 T-02 T-02 | 5/8 5/8 5/8 | 1/4 1/4 1/4 | 1/32 3/64 1/16 |  |  |  |   |  |
| CNG- 553 CNG- 553 CNG- 554 | CNGN 160712 CNGN 160712 CNGN 160716 | T-02 T-03 T-03 | 5/8 5/8 5/8 | 5/16 5/16 5/16 | 3/64 3/64 1/16 |  |  |    |   |  |
| CNG- 642 CNG- 643 CNG- 644 CNG- 648 | CNGN 190608 CNGN 190612 CNGN 190616 CNGN 190632 | T-02 T-02 T-02 T-02 | 3/4 3/4 3/4 3/4 | 1/4 1/4 1/4 1/4 | 1/32 3/64 1/16 1/8 |  |  |  |     |  |
| CNG- 653 CNG- 654 CNG- 658 | CNGN 190712 CNGN 190716 CNGN 190732 | T-02 T-02 T-02 | 3/4 3/4 3/4 | 5/16 5/16 5/16 | 3/64 3/64 1/16 |  |  |  |    |  |

CPG 80 diamond positive rake Insert 11 clearance

| Insert Number | ISO Designation | Specifications |  |  |  | Grades |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R |  | FMTCN |  |
| CPG-422 CPG-423 | CPGN 120308 CPGN 120312 | T-02 T-02 | 1/2 1/2 | 1/8 1/8 | 1/32 1/32 |  | ○ ○ |  |
| CPG-432 | CPGN 120408 | T-02 | 1/2 | 3/16 | 1/32 |  | ○ |  |

CNGA 80 diamond negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | H | FM 02 | FM73C | FM64C | FMY515 |
| CNGA-431 CNGA-432 | CNGA 120404 CNGA 120408 | T-02 T-02 | 3/8 3/8 | 3/16 3/16 | 1/64 1/32 | .150 .150 |   |   |   |   |
| CNGA- 433 CNGA- 434 | CNGA 120412 CNGA 120416 | T-02 T-02 | 1/8 | 3/16 | 1/32 | .203 |  |  |  |  |

DNG 55 diamond negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  | All Grades |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | FM02 | FM73C | FMY515 |
| DNG-432 DNG-433 | DNGN 150408 DNGN 150412 | T-02 T-02 | 1/2 1/2 | 3/16 3/16 | 1/32 3/64 |   |   | ○ ○ |
| DNG-442 DNG-443 DNG-444 | DNGN 150608 DNGN 150612 DNGN 150616 | T-02 T-02 T-02 | 1/2 1/2 1/2 | 1/4 1/4 1/4 | 1/32 3/64 1/16 |  |   | ○ ○  |
| DNG- 532 DNG- 533 | DNGN 190408 DNGN 190412 | T-02 T-02 | 5/8 5/8 | 3/16 3/16 | 1/32 3/64 |  | ○ ○ | ○ ○ |
| DNG -542 DNG- 543 DNG- 544 | DNGN 190608 DNGN 190612 DNGN 190616 | T-02 T-02 T-02 | 5/8 5/8 5/8 | 1/4 1/4 1/4 | 1/32 3/64 1/16 |  |    |  |

DNGA 55 diamond negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | H | FM 02 | FM 73C | FM 64C | FMY515 |
| DNGA-331 DNGA-332 | VNGA 151404 VNGA 151408 | T-02 T-02 | 3/8 3/8 | 3/16 3/16 | 1/64 1/32 | .150 .150 |   |   |   |   |
| DNGA- 432 | VNGA 151408 | T-02 | 1/8 | 3/16 | 1/32 | .203 |  |  |  |  |

RNG Negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  | All Grades |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | D | T | FM02 | FM73C | FMY515 |
| RNG-32 | RNGN 090300 | T-02 | 3/8 | 1/8 |  |  |  |
| RNG-42 RNG-43 RNG-45 | RNGN 120300 RNGN 120400 RNGN 120700 | T-02 T-02 T-02 | 1/2 1/2 1/2 | 1/32 3/64 1/16 |  |    | ○   |
| RNG- 55 RNG- 65 | RNGN 150700 RNGN 190700 | T-02 T-02 | 5/8 3/4 | 1/32 3/64 |  |   | ○ ○ |
| RNG -85 RNG- 86 | RNGN 250700 RNGN 250900 | T-02 T-02 | 1 1 | 5/16 5/8 |  |   |  ○ |

RPG positive rake Insert

| Insert Number | ISO Designation | Specifications |  |  | Grades |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | D | T |  | FMTCN |  |
| RPG-32 RPG-43 | RPGN 090300 RPGN 120400 | T-02 T-02 | 3/8 1/2 | 1/8 3/16 |  | ○ ○ |  |

RCGX positive rake Insert V bottom insert

| Insert Number | ISO Designation | Specifications |  |  | Grades |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C | T | FMAZ1 | FM AZ2 | FM AZ3 |
| RCGX-32 RCGX-43 |  | T-02 T-02 | 3/8 1/2 | 1/8 3/16 |  |   |   |

SNG Negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  | All Grades |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | FM02 | FM64C | FM73C | FM55C | FMY515 |
| SNG-322 | SNGN 090308 | T-01 | 3/8 | 1/8 | 1/32 |  |  |  |  |  |
| SNG-432 SNG-433 SNG-434 SNG-436 SNG-438 | SNGN 120408 SNGN 120412 SNGN 120416 SNGN-120424 SNGN-120432 | T-02 T-02 T-02 T-02 T-02 | 1/2 1/2 1/2 1/2 1/2 | 3/16 3/16 3/16 3/16 3/16 | 1/32 3/64 1/16 3/32 1/8 |      | ○ ○ ○ ○ ○ | ○ ○ ○ ○ ○ |      |      |
| SNG-452 SNG-453 SNG-454 | SNGN 120708 SNGN 120712 SNGN-120716 | T-02 T-02 | 1/2 1/2 1/2 | 5/16 5/16 5/16 | 1/32 3/64 1/16 |    |    |    |    |    |
| SNG-553 SNG-554 SNG-554 SNG-554 | SNGN 150712 SNGN 150716 SNGN 150716 SNGN 150724 | T-02 T-02 T-02 T-02 | 5/8 5/8 5/8 5/8 | 5/16 5/16 5/16 5/16 | 3/64 1/16 1/16 3/32 |   | ○ ○ ○ | ○ ○  |    | ○ ○ ○ ○ ○ |

SNGA Negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | D | FM02 | FM64C | FM73C | FMY515 |
| SNGA-322 | SNGA 090308 | T-02 | 3/8 | 1/8 | 1/32 | .150 |  |  |  |  |
| SNGA-432 SNGA-433 SNGA-434 | SNGA 120408 SNGA 120412 SNGA 120416 | T-02 T-02 T-02 | 1/2 1/2 1/2 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | .203 .203 .203 |    |    |    |    |

SPG Positive rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  | Grades |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | FM | FM | FM | FMTCN | FM |
| SPG-321 SPG-322 SPG-323 | SPGN 090304 SPGN 090308 SPGN 090312 | T-01 T-01 T-01 | 3/8 3/8 3/8 | 1/8 1/8 1/8 | 1/64 1/32 1/64 |  |  |  | ○ ○ ○ |  |
| SPR-421 SPR-422 SPR-423 | SPGN 120304 SPGN 120308 SPGN 312 | T-01 T-01 T-01 | 1/2 1/2 1/2 | 1/8 1/8 1/8 | 1/64 1/32 3/64 |  |  |  | ○ ○ ○ |  |
| SPG-433 SPG-434 | SPGN 120412 SPGN 120416 | T-02 T-02 | 1/2 1/2 | 3/16 3/16 | 3/64 1/16 |  |  |  | ○ ○ |  |

TNG Negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | B | FM 02 | FM64C | FM73C | FMY515 |
| TNG-222 | TNGN 110308 | T-02 | 1/4 | 1/8 | 1/32 | .3437 |  |  | ○ |  |
| TNG-322 | TNGN 160308 | T-02 | 3/8 | 1/8 | 1/32 | .5312 |  |  |  |  |
| TNG-332 TNG-333 TNG-334 | TNGN 160408 TNGN 160412 TNGN 160416 | T-02 T-02 T-02 | 3/8 3/8 3/8 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | .5312 .5156 .5000 |    |    |    |    |
| TNG- 352 TNG- 353 | TNGN 160708 TNGN 160712 | T-02 T-02 | 3/8 3/8 | 5/16 5/16 | 1/32 3/64 | .5312 .5156 |  |  |   |  |
| TNG-432 TNG-433 TNG-434 | TNGN 220408 TNGN 220412 TNGN 22-416 | T-02 T-02 T-02 | 1/2 1/2 1/2 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | .7188 .7031 .6875 |    |  |    |    |
| TNG- 453 TNG- 454 | TNGN 190608 TNGN 190612 | T-02 T-02 | 1/2 1/2 | 5/16 5/16 | 3/64 1/16 | .7031 .6875 |   |  |   |  |

TNGA Negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | H | B | FM 02 | FM 64C | FM 73C | FM |
| TNGA-322 | TNGA 090308 | T-02 | 3/8 | 1/8 | 1/32 | 0.150 | .5312 |  |  |  |  |
| TNGA-432 TNGA-433 TNGA-434 | TNGA 120408 TNGA 120412 TNGA 120416 | T-02 T-02 T-02 | 1/2 1/2 1/2 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | 0.203 0.203 0.203 | .7188 .7031 .6875 | ○   | ○ ○ ○ | ○ ○ ○ | ○ ○ ○ |

TP Positive rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  |  | Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | B | H | FM | FM | FMTCN | FM |
| TP-221 TP-222 TP-223 | TPGA 110304 TPGA 110308 TPGA 110312 | T-02 T-02 T-02 | 1/4 1/4 1/4 | 1/8 1/8 1/8 | 1/64 1/32 3/64 | .3675 .3438 .3281 | .150 .150 .150 |  |  |    |  |
| TP-321 TP-322 TP-323 | TPGA 160304 TPGA 160308 TPGA 160312 | T-01 T-01 T-01 | 3/8 3/8 3/8 | 1/8 1/8 1/8 | 1/64 1/32 3/64 | .5469 .5313 .5156 | .150 .150 .150 |  | ○ ○ ○ |    |   |

VNG 35 diamond negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | FM1 02 | FM 64C | FM 73C | FM Y515 |
| VNG-331 VNG-332 | VNG 160404 VNG 160408 | T-02 T-02 | 3/8 3/8 | 3/16 3/16 | 1/64 1/32 |   |   |   |   |
| VNG- 332 | VNG 190408 | T-02 | 1/8 | 3/16 | 1/32 |  | ○ |  | ○ |

VNGA 35 diamond negative rake Insert

| Insert Number | ISO Designation | Specifications |  |  |  |  | All Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | I.C. | T | R | H | FM 02 | FM 64C | FM 73C | FM Y515 |
| VNGA-331 VNGA-332 | VNGA 160404 VNGA 160408 | T-02 T-02 | 3/8 3/8 | 3/16 3/16 | 1/64 1/32 | .150 .150 |   |   |   |   |
| VNGA- 432 | VNGA 190408 | T-02 | 1/8 | 3/16 | 1/32 | .203 |  |  |  |  |

LNM Rectangle negative rake inserts

| Insert Number | ISO Designation | Specifications |  |  |  |  | Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | L | T | R | W | FMAZ1 | FM AZ2 | FM AZ3 | FM |
| LNM-222 |  | T-02 | 1-1/2 | 1/5 | 1/32 | .750 |  |  |  |  |
| LNM-322 |  | T-02 | 3/8 | 1/8 | 1/32 | .5312 |  |  |  |  |
| LNM-332 LNM-333 LNM-334 |  | T-02 T-02 T-02 | 3/8 3/8 3/8 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | .5312 .5156 .5000 |    |    |    |  |

ZT Precision ground

| Insert Number | ISO Designation | Specifications |  |  |  |  | Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | θ | L | T | R | W | FMAZ1 | FM AZ2 | FM AZ3 | FM |
| ZT967 ZT969 |  | 90o | 0.500 | .250 | 1/8 | .1187 |  | ○ |  |  |
| ZT-322 |  |  | 3/8 | 1/8 | 1/32 | .5312 |  |  |  |  |
| ZT-332 ZT-333 ZT-334 |  |  | 3/8 3/8 3/8 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | .5312 .5156 .5000 |    |    |    |    |

ZT Precision ground

| Insert Number | ISO Designation | Specifications |  |  |  |  | Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | θ | L | T | R | W | FMAZ1 | FM AZ2 | FM AZ3 | FM |
| ZT967 |  | 90o | 3/4 | 1/4 | 1/8 | 1/4 |  |  |  |  |
| ZT-322 |  |  | 3/8 | 1/8 | 1/32 | .5312 |  |  |  |  |
| ZT-332 ZT-333 ZT-334 |  |  | 3/8 3/8 3/8 | 3/16 3/16 3/16 | 1/32 3/64 1/16 | .5312 .5156 .5000 |    |    |    |  |

VDB

| Insert Number | ISO Designation | Specifications |  |  |  | Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | W | S | T | FMAZ1 | FM AZ2 | FM AZ3 | FM |
| VDB-222 |  | T-02 | 1/4 | 1/8 | 1/32 |  |  |  |  |
| VDB-322 |  | T-02 | 3/8 | 1/8 | 1/32 |  |  |  |  |
| VDB -332 VDB -333 VDB -334 |  | T-02 T-02 T-02 | 3/8 3/8 3/8 | 3/16 3/16 3/16 | 1/32 3/64 1/16 |    |    |    |  |

VDB-R

| Insert Number | ISO Designation | Specifications |  |  |  | Grades |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | E.P | W | S | T | FMAZ1 | FM AZ2 | FM AZ3 | FM |
| VDB-222 |  | T-02 | 1/4 | 1/8 | 1/32 |  |  |  |  |
| VDB-322 |  | T-02 | 3/8 | 1/8 | 1/32 |  |  |  |  |
| VDB 332 VDB -333 VDB -334 |  | T-02 T-02 T-02 | 3/8 3/8 3/8 | 3/16 3/16 3/16 | 1/32 3/64 1/16 |    |    |    |  |

| Material | Hardness | Operation | Grade | Median Cutting Speed, sfm (m/min) | Median Feed Rate, ipr | Depth of Cut Inches |
| --- | --- | --- | --- | --- | --- | --- |
| Carbon Steels | 100-250 BHN | Heavy Roughing | FMTCN | 1600 (480) | 0.014 | 0.120-0.500 |
|  |  | Roughing | FMAZ3 | 1600 (480) | 0.014 | 0.040-0.120 |
|  |  | Finishing | FMAZ1 | 2000 (600) | 0.008 | 0.012-0.040 |
|  |  | Fine Finishing | FMA | 2000 (600) | 0.004 | 0.004-0.020 |
| Carbon, Alloy & Tool Steels | 250-400 BHN | Heavy Roughing | FMTCN | 800 (240) | 0.014 | 0.120-0.500 |
|  |  | Roughing | FMAZ3 | 800 (240) | 0.014 | 0.040-0.120 |
|  |  | Finishing | FMAZ2 | 1250 (375) | 0.008 | 0.012-0.040 |
|  |  | Fine Finishing | FMAZ1 | 1250 (375) | 0.004 | 0.004-0.020 |
| Hardened Steel | 36 - 48 HRC | Roughing | FMTCN | 900 (270) | 0.008 | 0.120-0.200 |
|  |  | Finishing | FMAZ3 | 900 (270) | 0.008 | 0.120-0.200 |
|  | 50 - 56 HRC | Roughing | FMTCN | 600 (180) | 0.006 | 0.120 |
|  |  | Finishing | FMAZ3 | 600 (180) | 0.006 | 0.120 |
|  | 58 – 64 HRC | Finishing | FMAZ3 | 420 (125) | 0.004 | 0.040 |
| Chilled Cast Iron | 35 – 43 HRC | Roughing | FM02 | 450 (135) | 0.009 | 0.200 |
|  |  | Finishing | FM73C | 450 (135) | 0.009 | 0.200 |
|  | 46 –53 HRC | Roughing | FM02 | 300 (90) | 0.006 | 0.200 |
|  |  | Finishing | FM73C | 300 (90) | 0.006 | 0.200 |
|  | 56 – 62 HRC | Roughing | FM02 | 200 (60) | 0.004 | 0.200 |
|  |  | Finishing | FM64C | 200 (60) | 0.004 | 0.120 – 0.200 |
| Gray Cast Iron | 140 – 280 BHN | Heavy Roughing | FM02 | 1600 (480) | 0.016 | 0.120 – 0.500 |
|  |  |  | FM73C |  |  |  |
|  |  | Roughing | FM73C | 1600 (480) | 0.016 | 0.040 – 0.120 |
|  |  | Finishing | FM64C | 1800 (540) | 0.008 | 0.012 – 0.040 |
|  |  | Fine Finishing | FM55C | 1800 (540) | 0.004 | 0.004 – 0.020 |
| Nodular Cast Iron | 140 – 240 BHN | Heavy Roughing | FM02 | 950 (285) | 0.016 | 0.120 – 0.500 |
|  |  | Roughing | FM73C | 1050 (315) | 0.016 | 0.040 – 0.120 |
|  |  | Finishing | FM64C | 1350 (405) | 0.008 | 0.012 – 0.040 |
|  |  | Fine Finishing | FMYC | 1350 (405) | 0.004 | 0.004 – 0.020 |
| Black & White Malleable Cast Iron | 120 – 280 BHN | Heavy Roughing | FM02 | 950 (285) | 0.016 | 0.120 – 0.500 |
|  |  |  | FM73C |  |  |  |
|  |  | Roughing | FM02 | 1050 (315) | 0.016 | 0.040 – 0.120 |
|  |  | Finishing | FM55C | 1350 (405) | 0.008 | 0.012 – 0.040 |
|  |  | Fine Finishing | FMYC | 1350 (405) | 0.004 | 0.004 – 0.012 |

| Surface Speed SFM = .262 x DIA x RPM Revolutions Per Minutes RPM = 3.82 x SFM /DIA Feedrate (inches/minute) IPM = IPR x RPM Feed Rate (inches/revolution) IPR = t chip / cos α | Metal Removal Rate Q = 12 x DOC x IPR x SFM (in3/ min) Horsepower Required At The Spindle HPS = Q x UHP Horsepower Required At The Motor HPM = HPS / EFF Time In Cut (in seconds) T = 15.7 x DIA x LOC / SFM x IPR (sec) Or T = 60 x LOC / IPM (sec) |
| --- | --- |

Definition of Terms

DIA   = Diameter of the Workpiece (inches)

DOC = Depth of Cut (inches)

EFF   = Machine Efficiency

f        = Feed rate (see IPM and IPR)

HPM = Horsepower Required at the Motor (HP)

HPS   = Horsepower Required at the Spindle (HP)

IPM   = Feed rate (inches per minute)

IPR   = Feed rate (inches per revolution)

LOC = Length of Cut (inches)

Q       = Metal Removal Rate (cubic inches per minute)

RPM = Revolutions per Minute

SFM = Surface Feet per Minute

T       = Time (seconds)

t chip  = Chip Thickness (inches)

UHP = Unit Horsepower Factor

α       = Lead Angle

| Material | Hardness | Operation | Grade | Cutting Speed (SFM) |  |  | Feedrate (IPR) |  |  | Depth of Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | From | Median | To | From | Median | To |  |
| Steels, Carbon Contents 0.3 % or Less | 110 BHN | Heavy Roughing |  | 600 | 1,600 | 2,300 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 600 | 2,000 | 3,000 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 1,000 | 2,300 | 4,000 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 1,000 | 2,300 | 4,000 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 170 BHN | Heavy Roughing |  | 500 | 1,300 | 2,000 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 500 | 1,600 | 2,600 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 650 | 2,100 | 3,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 650 | 2,100 | 3,500 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 230 BHN | Heavy Roughing |  | 400 | 1,300 | 1,600 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 400 | 1,300 | 2,300 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 500 | 1,800 | 2,600 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 500 | 1,800 | 2,600 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 290 BHN | Heavy Roughing |  | 350 | 1,000 | 1,300 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 350 | 1,000 | 1,600 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 350 | 1,500 | 1,600 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 350 | 1,500 | 2,000 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 350 BHN | Heavy Roughing |  | 250 | 800 | 1,100 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 250 | 800 | 1,100 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 250 | 1,300 | 1,500 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 250 | 1,300 | 1,500 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 400 BHN | Heavy Roughing |  | 230 | 650 | 1,000 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 230 | 650 | 1,000 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 230 | 1,000 | 1,100 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 230 | 1,000 | 1,100 | 0.003 | - | 0.014* | 0.004 to 0.020 |

| Material | Hardness | Operation | Grade | Cutting Speed (SFM) |  |  | Feedrate (IPR) |  |  | Depth of Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | From | Median | To | From | Median | To |  |
| Steels, Carbon Content 0.35% or More | 110 BHN | Heavy Roughing |  | 600 | 2,000 | 2,300 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 650 | 2,000 | 2,600 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 650 | 2,300 | 3,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 650 | 2,300 | 3,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 170 BHN | Heavy Roughing |  | 500 | 1,600 | 2,000 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 500 | 1,600 | 2,300 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 500 | 2,100 | 2,600 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 500 | 2,100 | 2,600 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 230 BHN | Heavy Roughing |  | 400 | 1,300 | 1,600 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 400 | 1,300 | 2,000 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 400 | 1,800 | 2,000 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 400 | 1,800 | 2,000 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 290 BHN | Heavy Roughing |  | 350 | 1,000 | 1,300 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing |  | 350 | 1000 | 1,600 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing |  | 350 | 1,500 | 1,600 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing |  | 350 | 1,500 | 1,600 | 0.003 | - | 0.014* | 0.004 to 0.020 |

| Material | Hardness | Operation | Grade | Cutting Speed (SFM) |  |  | Feedrate (IPR) |  |  | Depth of Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | From | Median | To | From | Median | To |  |
| Steels, Carbon Content 0.35% or More | 350 BHN | Heavy Roughing | FMAZ3 | 250 | 800 | 2,300 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing | FMAZ3 | 250 | 800 | 2,600 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing | FMAZ2 | 250 | 1,300 | 3,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMA | 250 | 1,300 | 3,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 400 BHN | Heavy Roughing | FMAZ3 | 230 | 650 | 1,000 | 0.012 | 0.014 | 0.024 | 0.120 to 0.500 |
|  |  | Roughing | FMAZ3 | 230 | 650 | 1,000 | 0.012 | 0.014 | 0.024 | 0.040 to 0.120 |
|  |  | Finishing | FMAZ2 | 230 | 1,000 | 1,100 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMAZ! | 230 | 1,000 | 1,100 | 0.003 | - | 0.014* | 0.004 to 0.020 |
| Hardened Steels (36 to 64 HRC) | 36 HRC | Roughing Finishing | FMAZ3 FMAZ1 | 300 | 1,050 | 1,300 |  | 0.014 max** |  | 0.200 |
|  | 42 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 260 | 900 | 1,150 |  | 0.011 max** |  | 0.200 |
|  | 48 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 230 | 750 | 980 |  | 0.008 max** |  | 0.120 |
|  | 52 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 200 | 660 | 800 |  | 0.007 max** |  | 0.12 |
|  | 56 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 170 | 550 | 650 |  | 0.006 max** |  | 0.120 |
|  | 60 HRC | Finishing | FMAZ3 FMAZ3 | 140 | 450 | 550 |  | 0.005 max** |  | 0.040 |
|  | 64 HRC | Finishing | FMAZ3 FMAZ3 | 100 | 380 | 450 |  | 0.004 max** |  | 0.040 |
| Chilled Cast Irons | 35 HRC | Roughing Finishing | FMAZ3 FMAZ1 | 390 | 520 | 790 |  | 0.011 max** |  | 0.200 |
|  | 40 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 330 | 460 | 720 |  | 0.010 max** |  | 0.200 |
|  | 43 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 300 | 390 | 660 |  | 0.009 max** |  | 0.200 |
|  | 46 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 250 | 330 | 590 |  | 0.008 max** |  | 0.200 |
|  | 50 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 200 | 290 | 520 |  | 0.007 max** |  | 0.200 |
|  | 53 HRC | Roughing Finishing | FMAZ3 FMAZ3 | 170 | 260 | 460 |  | 0.006 max** |  | 0.200 |
|  | 56 HRC | Roughing Finishing | FMAZ3 FMAZ3 | 150 | 230 | 390 |  | 0.006 max** |  | 0.200 |
|  | 59 HRC | Roughing Finishing | FMAZ3 FMAZ1 | 130 | 200 | 330 |  | 0.005 max** |  | 0.200 |
|  | 62 HRC | Roughing Finishing | FMAZ3 FMAZ2 | 100 | 160 | 260 |  | 0.004 max** |  | 0.200 |

| Material | Hardness | Operation | Grade | Cutting Speed (SFM) |  |  | Feedrate (IPR) |  |  | Depth of Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | From | Median | To | From | Median | To |  |
| Gray Cast Irons | 140 to 210 BHN | Heavy Roughing** | FM02 | 650 | 1,600 | 2,600 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 650 | 2,000 | 3,300 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FMYC | 650 | 2,300 | 3,900 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 650 | 2,300 | 3,900 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 220 to 240 BHN | Heavy Roughing** | FM02 | 650 | 1,300 | 2,000 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 650 | 1,600 | 2,000 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FMYC | 650 | 1,700 | 2,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 650 | 1,700 | 2,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 250 to 280 BHN | Heavy Roughing** | FM02 | 350 | 1,000 | 1,300 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 350 | 1,100 | 1,300 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FM64C | 500 | 1,200 | 1,500 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 500 | 1,200 | 1,500 | 0.003 | - | 0.014* | 0.004 to 0.020 |
| Nodular Cast Irons | 140 BHN | Heavy Roughing | FM02 | 650 | 1,100 | 1,300 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing | FM73C | 650 | 1,300 | 1,800 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FM64C | 800 | 1,600 | 2,000 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 800 | 1,600 | 2,000 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 190 BHN | Heavy Roughing | FM02 | 650 | 1,100 | 1,300 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing | FM64C | 650 | 1,300 | 1,800 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FMYC | 1,000 | 1,600 | 1,800 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 1,000 | 1,600 | 1,800 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 240 BHN | Heavy Roughing | FM02 | 350 | 800 | 1,150 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing | FM64C | 350 | 800 | 1,150 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FMYC | 500 | 1,150 | 1,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 500 | 1,150 | 1,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |

| Material | Hardness | Operation | Grade | Cutting Speed (SFM) |  |  | Feedrate (IPR) |  |  | Depth of Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | From | Median | To | From | Median | To |  |
| Black Malleable Cast Irons | 140 to 190 BHN | Heavy Roughing** | FM02 | 650 | 1,600 | 2,600 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 650 | 2,300 | 3,300 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FM64C | 650 | 2,300 | 3,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FM55C | 650 | 2,300 | 3,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 200 to 250 BHN | Heavy Roughing** | FM02 | 650 | 1,300 | 2,000 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 650 | 1,600 | 2,000 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FM64C | 650 | 1,600 | 2,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 650 | 1,600 | 2,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 260 to 290 BHN | Heavy Roughing** | FM02 | 350 | 1,000 | 1,300 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM02 | 350 | 1,000 | 1,300 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FMYC | 350 | 1,100 | 1,500 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 350 | 1,100 | 1,500 | 0.003 | - | 0.014* | 0.004 to 0.020 |
| White Malleable Cast Irons | 120 to 190 BHN | Heavy Roughing** | FM02 | 650 | 1,600 | 2,600 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 650 | 2,000 | 3,300 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FM64C | 650 | 2,300 | 3,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FM55C | 650 | 2,300 | 3,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 200 to 250 BHN | Heavy Roughing** | FM02 | 650 | 1,300 | 2,000 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM73C | 650 | 1,600 | 2,000 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FM64C | 650 | 1,600 | 2,300 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 650 | 1,600 | 2,300 | 0.003 | - | 0.014* | 0.004 to 0.020 |
|  | 260 to 290 BHN | Heavy Roughing** | FM02 | 350 | 1,000 | 1,300 | 0.010 | 0.016 | 0.028 | 0.120 to 0.625 |
|  |  | Roughing** | FM02 | 350 | 1,00 | 1,800 | 0.010 | 0.016 | 0.028 | 0.040 to 0.120 |
|  |  | Finishing | FMYC | 350 | 1,100 | 1,500 | 0.008 | - | 0.060* | 0.012 to 0.040 |
|  |  | Fine Finishing | FMYC | 350 | 1,100 | 1,500 | 0.003 | - | 0.014* | 0.004 to 0.020 |

| Material | Hardness | Operation | Grade | Cutting Speed (SFM) |  |  | Feedrate (IPR) |  |  | Depth of Cut |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | From | Median | To | From | Median | To |  |
| High Temperature Nickel Base Alloys** Inconel 600 Series, Monel | 115 BHN | Roughing | FMYC | 500 | 800 | 1,000 | 0.005 | 0.006 | 0.010 | 0.150 |
|  |  | Semifinishing | FMYC | 600 | 900 | 1,200 | 0.005 | 0.006 | 0.010 | 0.060 |
|  | 200 BHN | Roughing | FMYC | 500 | 700 | 900 | 0.004 | 0.006 | 0.008 | 0.150 |
|  |  | Semifinishing | FMYC | 600 | 800 | 1,000 | 0.004 | 0.006 | 0.008 | 0.060 |
|  | 360 BHN | Roughing | FMYC | 300 | 500 | 700 | 0.004 | 0.006 | 0.008 | 0.150 |
|  |  | Semifinishing | FMYC | 400 | 600 | 800 | 0.004 | 0.006 | 0.008 | 0.060 |
| Inconel 700 Series Waspalloy | 360 BHN | Roughing | FMYC | 500 | 800 | 1,100 | 0.005 | 0.006 | 0.010 | 0.100 |
|  |  | Semifinishing | FMYC | 600 | 900 | 1,200 | 0.005 | 0.006 | 0.010 | 0.060 |
|  | 450 BHN | Roughing | FMYC | 300 | 700 | 900 | 0.004 | 0.006 | 0.008 | 0.100 |
|  |  | Semifinishing | FMYC | 400 | 800 | 1,000 | 0.004 | 0.006 | 0.008 | 0.060 |
| Hastelloy, Rene | 300 BHN | Roughing | FMYC | 300 | 500 | 700 | 0.003 | 0.005 | 0.008 | 0.100 |
|  |  | Semifinishing | FMYC | 400 | 600 | 800 | 0.003 | 0.005 | 0.008 | 0.060 |
|  | 375 BHN | Roughing | FMYC | 250 | 400 | 500 | 0.002 | 0.004 | 0.006 | 0.075 |
|  |  | Semifinishing | FMYC | 300 | 500 | 600 | 0.002 | 0.004 | 0.006 | 0.060 |

Ten Suggestions for the Ceramic User

The properties of ceramic-based cutting materials are completely different from conventional materials, such as cemented carbides and high-speed steel. These are ten basic recommendations for the application of ceramic cutting tools:

- Best efficiency with ceramic cutting tools is achieved in large quantity metal removal operations, in the machining of hard materials and in the machining of large work pieces.

- Best efficiency with ceramic cutting tools is achieved with the highest cutting speeds possible and with square or round indexable inserts.

- Rigid machine tools, safe clamping devices and rigid workpieces are recommended for machining with ceramic cutting tools.

- Clutches and brakes of the machine tool should be designed for “higher operating frequency” or shorter machining cycles.

- Chip conveyors, capable of handling large amounts of chips (20 lbs per minute, minimum), should be attached to the machine tool.

- Gain experience with ceramic cutting tools by machining materials with good machinability, such as grey cast iron or carbon steel. Do not expect immediate solutions for exotic materials or complex workpieces.

- The conversion to ceramic cutting tools requires a review of the machining sequence. At the entry point of the cutting edge, a precut chamfer or a reduced feedrate is recommended.

- Machine operators need adequate training to accept the highly productive ceramic cutting tools.

- Machining parameter should be precisely specified to prevent misapplications.

- Coolants are NOT required, except when machining high temperature alloys.

| Maximum Feedrate for Turning 1045 (200 BHN) With Ceramic Inserts |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Toolholder | Side Cutting Edge Angle | Cutting Edge Angle | Nose Radius |  |  |  |  | Protective Chamfer |
|  |  |  | 5 | 4 | 3 | 2 | 1 |  |
| CSSN | 45º | 90º | 0.022 | 0.020 | 0.014 | 0.010 | 0.006 | T00820 |
| CSRN | 15º | 90º | 0.015 | 0.014 | 0.011 | 0.007 | 0.007 | T00820 |
| CCLN | -5º | 80º | 0.014 | 0.013 | 0.010 | 0.006 | 0.006 | T00820 |
| CDJN | -3º | 55º | 0.010 | 0.009 | 0.007 | 0.005 | 0.005 | T00820 |

| Maximum Feedrate for Turning 1045 (180 BHN) With Ceramic Inserts |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Toolholder | Side Cutting Edge Angle | Cutting Edge Angle | Nose Radius |  |  |  |  | Protective Chamfer |
|  |  |  | 5 | 4 | 3 | 2 | 1 |  |
| CSSN | 45º | 90º | 0.025 | 0.022 | 0.016 | 0.011 | 0.007 | T00820 |
| CSRN | 15º | 90º | 0.018 | 0.016 | 0.012 | 0.008 | 0.006 | T00820 |
| CCLN | -5º | 80º | 0.016 | 0.014 | 0.011 | 0.007 | 0.005 | T00820 |
| CDJN | -3º | 55º | 0.011 | 0.010 | 0.008 | 0.006 | 0.003 | T00820 |

For the machining of chilled cast iron and hardened ferrous metals, the selection of the correct chip thickness relative to the hardness is extremely important. The application of round inserts requires close control of the feedrate. When turning with round inserts, the undeformed chip will have a shape as shown in the picture below:

| Table 1 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Hardness |  |  |  | Recommended Maximum Chip Thickness ( tchip) |
| Brinell | Shore C | Vickers | Rockwell |  |
| 225 | 34 | 237 | 20 | 0.014 |
| 255 | 38 | 266 | 25 | 0.013 |
| 285 | 42 | 302 | 30 | 0.012 |
| 325 | 48 | 345 | 35 | 0.011 |
| 370 | 54 | 390 | 40 | 0.010 |
| 400 | 57 | 425 | 43 | 0.009 |
| 480 | 67 | 513 | 50 | 0.008 |
| 525 | 71 | 560 | 53 | 0.007 |
| 580 | 73 | 613 | 56 | 0.006 |
| 635 | 80 | 674 | 59 | 0.005 |
| 690 | 85 | 746 | 62 | 0.004 |

| Table 2 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Depth of Cut | Factor M for Round Inserts With Various I.C. |  |  |  |  |  |  |
|  | 1/4 | 3/8 | 1/2 | 5/8 | 3/4 | 1 | 1 1/4 |
| 0.012 | 2.3 | 2.8 | 3.3 | 3.6 | 4.0 | 4.6 | 5.1 |
| 0.020 | 1.8 | 2.2 | 2.6 | 2.8 | 3.1 | 3.6 | 4.0 |
| 0.040 | 1.4 | 1.6 | 1.8 | 2.0 | 2.2 | 2.6 | 2.8 |
| 0.060 | ___ | 1.4 | 1.5 | 1.7 | 1.8 | 2.1 | 2.3 |
| 0.080 | ___ | ___ | 1.4 | 1.5 | 1.6 | 1.8 | 2.0 |
| 0.120 | ___ | ___ | ___ | 1.3 | 1.4 | 1.5 | 1.7 |
| 0.160 | ___ | ___ | ___ | ___ | ___ | 1.4 | 1.5 |

| Surface Speed SFM = .262 x DIA x RPM Revolutions Per Minute RPM = 3.82 x SFM / DIA Feedrate (inches/minute) IPM = IPR x RPM Chip Thickness IPR = tchip | Metal Removal Rate Q = 12 x WOC x IPR x SFM (in3/min) Horsepower Required At The Spindle HPS = Q x UHP Horsepower Required At The Motor HPM = HPS/EFF Time In Cut (in seconds) T= 7.85 x DOC x (DIA + DIAG)/ SFM x IPR (sec) Or T = 60 x DOC / IPM (sec) |
| --- | --- |

Definition of Terms

DIA = Diameter of the Workpiece (inches)

DIAG = Diameter of Groove (inches)

(see figures above for details)

DOC = Depth of Cut (inches)

EFF = Machine Efficiency

f = Feedrate (see IPM and IPR)

HPM = Horsepower Required at the Motor (HP)

HPS = Horsepower Required at the Spindle

IPM = Feedrate (inches per minute)

IPR = Feedrate (inches per revolution)

Q = Metal Removal rate (cubic inches per minute)

RPM = Revolutions per Minute

SFM = Surface Feet per Minute

T = Time (seconds)

tchip =  Chip Thickness (inches)

UHP = Unit Horsepower Factor

WOC = Width of Cut or Groove Width (inches)

For optimal application of the ceramic cutting tools, the edge preparation should be adjusted to the cutting tool material, the work-piece material and the machining operation being applied. The edge preparation of ceramic cutting tools consists of designing a chamfer or a hone. The chamfer is defined by the width (W) and the angle (), while the hone is defined only by the radius (r).

Chamfer                                                                                 Hone

Width (W)

R

Angle ()

Three standard chamfer sizes are designed:

| Designation | Width (W) | Angle () |
| --- | --- | --- |
| T-01 T-02 T-03 | 0.003” 0.008” 0.012” | 20 25 30 |